## Slide 1
Fridge set-up and packaging
Fully coaxial Quantum Socket (DC-8GHz)
  ~ 150mΩ contact resistance
  ~ 10Ω impedance mismatch
56dB attenuation on measurement line
SucoFlex, flexible cables and
EZ Form SemiRigid
Semi rigid CoaxCo
SC-219/50-SS-SS
Semi rigid
EZ 86-Cu-TP/M17
Semi rigid
SC-219/50-
Nb-Nb
Semi rigid CoaxCo
SC-219/50-SS-SS
J.H. Béjanin... M. Mariantoni,
Phys. Rev. Applied 6, 044010 (2016)
Notes: fridge set-up including wiring attenuation, thermalization, and sample mounting, and

## Slide 2
Unprocessed
RCA1 + HF
RCA1 + HF
+ 880C Anneal
880C Anneal
Alternative annealing recipes
Fabrication
Basic fabrication steps
Chemical clean and thermal anneal
UHV Al deposition
UV lithography
Chlorine based ICP etch
Potential issues
Annealing creates trade-off between oxide removal and surface roughness
Need to explore full recipe space more (one resonator on very rough 950C sample very good)
Resonators fabbed on chip with JJ are much worse, even if not exposed to ion mill
C.T. Earnest... M. Mariantoni, Supercond. Sci. Technol. 31, 125013 (2018)

## Slide 3
Surface Treatment | F tanδ | Qi nph ~ 1
Unprocessed | 3.27 E-6 | 320 000
RCA1 – HF | 1.53 E-6 | 530 000
880C Anneal | 1.56 E-6 | 560 000
RCA1 + HF + 880C Anneal | 0.80 E-6 | 820 000
High Power Quality Crossovers
Small (<5μT) field can impact 1/Qi by order of magnitude (B.Chiaro, 2016)
Cleaner Al films more susceptible than dirty films to quality loss from magnetic fields
(S Kwon, 2018)
Plotting standardization: Q or 1/Q?
Resonator measurements
S-curve fit obtained from modified TLS model with α between 0.24 - 0.33
Mean photon number estimated. Pin is rough and does not account for frequency
Notes: resonator measurements, data analysis, and modelling.

## Slide 4
fit the normalization data in magnitude and phase separately to a line;
extrapolate the value of the magnitude and phase in the frequency range of the resonator data;
subtract the extrapolated data from the resonator data in the complex plane. This has the effect of de-embedding the measurement setup from the data.
invert the normalized resonator data;
fit the inverted normalized resonator data to (A.1) (A.Megrant, 2012) using standard nonlinear least squares techniques, starting from a reasonable initial parameters choice;
calculate the fitting errors from the covariance matrix;
obtain the fitting parameters and associated errors.
(A.1)
Resonator fitting
Notes: Photon estimation

## Slide 5
Geometry/Participation Ratios
Hard to compare Qi across publications
Determining filling factor relies on simulations: reproducible across simulation platform? At least for very simple/similar geometries
Simulations are unstable w.r.t. small reasonable parameter change: oxide thickness, conductor edge sharpness, surface roughness
STANDARDIZATION: Choose a common set of designs (lumped element and CPW)

## Slide 6
Fitting to TLS Model for low Tc material
Quasiparticle effects take over too quickly, can’t see temperature dependence of TLS loss
Fitting to TLS model at low power
At low power , Qi and f0 fluctuations are large, need many measurements to average but fluctuations over long times are also large
Extra fitting parameters: α
Deviates from expected value of 0.5
TLS Model difficulties
Notes: Note from Chalmers

## Slide 7
Fabrication TEM – BKP 1

## Slide 8: The Pocketmon Qubit – BKP2
E.A. Peters and M. Mariantoni, in preparation
Copyright Matteo Mariantoni 2017
Vacuum-gap capacitor
G

## Slide 9: Metal-Oxide Participation Decreases Inversely with Capacitor Gap – BKP3
Metal oxide filling factor depends on and :